A fiber Patch Cord is a connector plug installed at both ends of the fiber optic cable to enable optical connection, and a plug at one end is called a tail fiber. Optical Fiber Patch Cord/Cable is similar to coaxial cables, but does not have a mesh shield. The center is the glass core of light propagation.

| Features |  |
| --- | --- |
| Low Insertion Loss High Return Loss Good Mechanics High Stability and Reliability |  |
| Application |  |
| FTTH / CATV System The Field of Optical Communication Optical Transmission System Equipment Tester |  |

Performance Specifications

| Parameters | Unit | FC, SC, LC | ST, MU | MTRJ |
| --- | --- | --- | --- | --- |
|  |  | SM | MM | SM | MM | SM | MM |
|  |  | UPC | APC | UPC | APC | UPC | UPC | UPC | UPC |
| Operating Wavelength | nm | 1310,1550 | 850,1300 | 1310,1550 | 850,1300 | 1310,1550 | 850,1300 |
| Insertion Loss | dB | ≤0.3 | ≤0.3 | ≤0.3 | ≤0.3 | ≤0.3 | ≤0.3 | ≤0.3 |
| Return Loss | dB | ≥55 | ≥60 | ≥35 | ≥50 | ≥35 | ≥50 | ≥35 |
| Repeatability | dB | ≤0.1 |
| Interchangeability | dB | ≤0.2 |
| Number of times of plug and pull | Times | ≥1000 |
| Operating Temperature | ℃ | -10~+70 |
| Storage Temperature | ℃ | -40~+85 |

Core Technical Parameters

| Mode | Single Mode | Multi Mode |
| --- | --- | --- |
| Length | 10.50±0.05mm | 10.50±0.05mm |
| Outer Diameter | 2.4990±0.0005mm | 2.4990±0.0005mm |
| Inner diameter | 0.125±0.001/-0mm | 0.126-0.129mm |
| Concentricity | ≤1.0 | ≤4.0 |

Order information: